**GENERAL TITANIUM DIOXIDE KY6618**

Characteristics

KY6618 is a zirconium ,aluminum and organic surface treated multipurpose rutile titanium dioxide pigment ,it has average particle size distribution,good whiteness,good dispersion,high gloss,good hiding powder and high weather resistance properties .It is widely used in coating ,paints,ink,leather,rubber and ink production.

|  |  |
| --- | --- |
| Quality index | Technical requirement |
| The content of titanium dioxide ,%) | ≥93.50 |
| Surface treated | Zirconium,aluminum |
| Brightness,% | ≥97% |
| Oil absorption ,g/100g | ≤20 |
| L value | ≥97.00 |
| B value | ≤2.00 |
| Tinting Strength ,% | ≥105 |
| Residue on sieve (45 μm),% | ≤0.02 |
| Resistivity,Ω·m | ≥60 |

**Application fields:**

1.Coating

2.Ink(Solvent-based,tin-printing)

3.Leather ,color paste and sheet

4.Paints

5.Plastic

6.Rubber

**Packing :**

1.25kg paper-plastic composite bag

2.1000kg ton bag

**Remarks**

Product index will be subject to inspection report.